CURRICULUM EMBEDDED PERFORMANCE TASK MATRIX—NINTH GRADE HIGH SCHOOL SCIENCE (CAPT)

| PARAMETER | STRAND I: ENERGY TRANSFORMATIONS | STRAND II: CHEMICAL STRUCTURES AND PROPERTIES | STRAND III: GLOBAL INTERDEPENDENCE |
| --- | --- | --- | --- |
| EMBEDDED TASK TITLE | SOLAR COOKER | SYNTHETIC POLYMERS | ACID RAIN |
| YOUR TASK | You and your lab partner will design and conduct an experiment to investigate one factor that contributes to the effectiveness of solar cooker in heating water. Factors you may want to investigate include: the shape of the collector, the shape of the water container, orientation of the collector, surface area of the collector, or the color of the collector. | You and your lab partner will design an experiment that investigates a stress-strain behavior among various plastic products made of the synthetic polymer polyethylene. | Your town council is commissioning a new statue to be displayed downtown. You and your lab partner will conduct an experiment to investigate the effect of acid rain on various building materials in order to make a recommendation to the town council as to the best material to use for the statue. In your experiment, vinegar (pH ( 3) will simulate acid rain. |
| RESEARCH QUESTION | Of black (≈ tar), brown (≈ soil), green (≈ vegetation), and beige (≈ sand) which color solar cooker will have the highest final temperature? | The Drop Dart Test Of Name Brand Plastic Wrap #1, Name Brand Plastic Wrap #2, and Generic Store Brand Plastic Wrap which polyethylene wrap will have highest puncture resistance? | Of marble, pea stone, red sandstone, and granite, which material is the BEST for building a weather resistant statute? |
| HYPOTHESIS/PREDICTION | If black, brown, green, and beige lined solar cookers are subjected to direct sunlight, then the black solar cooker will have the greatest increase in temperature because black absorbs the most energy. | If a (120 g dart (i.e., long bolt) is dropped from varying heights (cm), then the Generic Plastic Wrap will exhibit the least puncture resistance [mass (g) x height (cm)] because it is the least expensive. | If marble, pea stone, red sandstone, and granite are subjected to acid rain (pH ( 3) then granite will deteriorate the least because it is the most resistant to weathering |
| PARAMETER | STRAND I: ENERGY TRANSFORMATIONS | STRAND II: CHEMICAL STRUCTURES AND PROPERTIES | STRAND III: GLOBAL INTERDEPENDENCE |
| EMBEDDED TASK TITLE | SOLAR COOKER | SYNTHETIC POLYMERS | ACID RAIN |
| EXPERIMENT INDEPENDENT VARIABLE | The color (black, brown, green, and beige) of the paper lining the solar cooker. | Drop Dart Test Height (cm) | Type of building material (marble, pea stone, red sandstone, or granite) |
| EXPERIMENT DEPENDENT VARIABLE | The increase in temperature of the water in (C. | Puncture Resistance (g x cm) | % of Mass Remaining |
| CONTROL EXPERIMENT | Instead of colored construction paper line the solar cooker with white construction paper. | N/A | Instead of acid rain test (submerge) the building materials (marble, pea stone, red sandstone, and granite) in tap (pure) water with a pH of ( 7 |
| VARIABLES THAT MUST BE KEPT CONSTANT | Shape and size of the solar collector, orientation of the solar cooker toward the sun, surface area of the colored paper inside the solar cooker, angle of the solar collector to the sun (i.e., 90() same reflective surface (aluminum foil), and the same thickness of Saran Wrap to let the light into and trap the heat. | Same dart (i.e., the same mass in g), same surface area of plastic wrap, same person securing the plastic, same angle of drop (i.e., perpendicular to plastic), and the same gravity (just drop the dart; do not throw or propel it in any way). | Same amount of time in the vinegar (24 hours), same amount of vinegar (100 mL), same mass of building material (20 g), same balance, same brand of vinegar, and same size container/lid |